TR-TPO

产品简介 General Information

- TR-TPO是一款通用型自由基光引发剂，具备较长的吸收波长、优秀的深层固化性能、光漂白性，特别适用于LED涂料和油墨中使用。

- TR-TPO is a general free radical photoinitiator with long absorption wavelength, excellent deep curing performance and photo-bleaching property. It is particularly suitable for LED curing coatings and inks.

产品信息 Product Information

- 化学名称 Chemical Name：2,4,6-三甲基苯甲酰二苯氧膦 Diphenyl(2,4,6-trimethylbenzoyl) phosphine oxide

- 分子量 Molecular Weight：348.38

- CAS No：75980-60-8

紫外吸收光谱 UV Absorbance Spectrum

技术参数 Technical Parameters

- 外观 Appearance：淡黄色粉末 Light yellow powder

- 纯度 Purity (HPLC)：≥98.00%

- 熔程 Melting Range：85.0~95.0ºC

产品优势 Benefits

- 长吸收波长 Long absorption wavelength

- 优秀的深层固化性能 Excellent deep curing performance

- 光漂白性，抗黄变 Good yellow resistance and photo-bleaching property

应用 Applications

- TR-TPO由于在LED固化领域中优良的性能，被广泛应用于光固化涂料和油墨。当和TR-184协同使用时能够获得更平衡的性能表现。涂料中的建议添加量约为1~3%，油墨中的建议添加量约为5~10%。

- TR-TPO is widely used in coating and ink due to its excellent performance in LED curing. It can achieve more balanced performance when used with TR-184. The recommended addition amount in coating is about 1~3%, and that in ink is about 5~10%.

存储及包装 Storage & Packaging

- 保存在密闭容器中储存在阴凉、干燥、阴暗、通风的区域。自生产日期开始，1年内有效。包装：20kg/箱。

- Keep in a tightly closed container and store in a cool, dry, dark, ventilated area. Effective from the date of production, within 1 year. Packaging: 20kg/carton.

THE END