TR-NPI-20401

产品简介 General Information

- TR-NPI-20401是一款通用型自由基光引发剂，具备高引发活性和优秀的深层固化性能，具备无生殖毒性、低气味、低迁移的特性，以及良好的溶解性和优秀的热稳定性，是TR-NPI-20400的性能改进版本，常作为TR-907的替代品使用。TR-NPI-20401可与其他光引发剂搭配使用，尤其是和硫杂蒽酮协同使用时特别适用于有色体系的光固化。

- TR-NPI-20401 is a general free radical photoinitiator with high initiating activity and excellent deep curing performance, as well as non-reproductive toxic, low odor, low migration, good solubility, excellent thermal stability. It’s improved product of TR-NPI-20400, usually used as a substitute for TR-907. TR-NPI-20401 can be used in combination with other photoinitiators, especially suitable for colored curing when used with thioxanthone.

产品信息 Product Information

- 化学名称 Chemical Name：保密 Confidential

- 分子量 Molecular Weight：保密 Confidential

- CAS No：无资料 Not available

紫外吸收光谱 UV Absorbance Spectrum

技术参数 Technical Parameters

- 外观 Appearance：类白色至淡黄色粉末 Off-white to light yellow powder

- 纯度 Purity (HPLC)：≥98.50%

产品优势 Benefits

- 极高的反应活性 Excellent initiating activity

- 长吸收波长 Long absorption wavelength

- 无生殖毒性、低气味、低迁移 Non reproductive toxic, low odor, low migration

- 良好的溶解性 Good solubility

- 优秀的热稳定性 Excellent thermal stability

- 优秀的深层固化性能 Excellent deep curing performance

应用 Applications

- TR-NPI-20401可用于直接替代TR-907，建议添加量为3~5%。当和硫杂蒽酮协同使用时，例如TR-DETX，特别适用于有色体系的光固化。

- TR-NPI-20401 can be used to directly replace TR-907. The usual recommended dosage is 3~5%. It’s especially suitable for colored system when used with thioxanthone as TR-DETX.

存储及包装 Storage & Packaging

- 保存在密闭容器中储存在阴凉、干燥、阴暗、通风的区域。自生产日期开始，2年内有效。包装：20kg/桶。

- Keep in a tightly closed container and store in a cool, dry, dark, ventilated area. Effective from the date of production, within 2 years. Packaging: 20kg/drum.

THE END