TR-NPI-705

产品简介 General Information

- TR-NPI-705是一款混合型自由基光引发剂，具备较长的吸收波长、优秀的深层固化性能、光漂白性，特别适用于LED涂料和油墨中使用。

- TR-NPI-705 is a mixed free radical photoinitiator with long absorption wavelength, excellent deep curing performance and photo-bleaching property. It is particularly suitable for LED curing coatings and inks.

产品信息 Product Information

- 化学名称 Chemical Name：2,4,6-三甲基苯甲酰二苯氧膦 Diphenyl(2,4,6-trimethylbenzoyl) phosphine oxide

2-羟基-2-甲基-1-苯基丙酮 2-Hydroxy-2-methyl-1-phenyl-1-propanone

- CAS No：75980-60-8, 7473-98-5

技术参数 Technical Parameters

- 外观 Appearance：淡黄色透明液体 Light yellow transparent liquid

- 纯度 Purity (HPLC)：≥98.00%

产品优势 Benefits

- 长吸收波长 Long absorption wavelength

- 优秀的深层固化性能 Excellent deep curing performance

- 光漂白性，抗黄变 Good yellow resistance and photo-bleaching property

应用 Applications

- TR-NPI-705由于在LED固化领域中优良的性能，被广泛应用于光固化涂料和油墨。建议添加量约为5~10%。

- TR-NPI-705 is widely used in coating and ink due to its excellent performance in LED curing. The recommended addition amount is about 5~10%.

存储及包装 Storage & Packaging

- 保存在密闭容器中储存在阴凉、干燥、阴暗、通风的区域。自生产日期开始，1年内有效。包装：20kg/桶。

- Keep in a tightly closed container and store in a cool, dry, dark, ventilated area. Effective from the date of production, within 1 year. Packaging: 20kg/Pail.

THE END