TR-NPI-601

产品简介 General Information

- TR-NPI-601是一款通用型自由基光引发剂，具备高固化活性、较长的吸收波长、优秀的深层固化性能、光漂白性，特别适用于LED涂料和油墨中使用。

- TR-NPI-601 is a general free radical photoinitiator with high curing activity, long absorption wavelength, excellent deep curing performance, and photo-bleaching property. It is particularly suitable for LED curing coatings and inks.

产品信息 Product Information

- 化学名称 Chemical Name：苯基双(2,4,6-三甲基苯甲酰基)氧化膦 Bis(2,4,6-trimethylbenzoyl) phenylphosphine oxide

- 分子量 Molecular Weight：418.46

- CAS No：162881-26-7

紫外吸收光谱 UV Absorbance Spectrum

技术参数 Technical Parameters

- 外观 Appearance：淡黄色粉末 Light yellow powder

- 纯度 Purity (HPLC)：≥98.00%

- 干燥失重 Loss on Drying：≤0.50%

- 熔程 Melting Range：127~135ºC

产品优势 Benefits

- 优秀的引发活性 High curing activity

- 长吸收波长 Long absorption wavelength

- 优秀的深层固化性能 Excellent deep curing performance

- 光漂白性，抗黄变 Good yellow resistance and photo-bleaching property

应用 Applications

- TR-NPI-601通常作为TR-TPO的活性改良版本使用，在实际应用中两种引发剂经常搭配使用。建议添加量约为1~3%。

- TR-NPI-601 is usually used as a better activity version of TR-TPO, and the two initiators are often used together in practical applications. The recommended addition amount is about 1~3%.

存储及包装 Storage & Packaging

- 保存在密闭容器中储存在阴凉、干燥、阴暗、通风的区域。自生产日期开始，18个月内有效。包装：20kg/箱。

- Keep in a tightly closed container and store in a cool, dry, dark, ventilated area. Effective from the date of production, within 18 months. Packaging: 20kg/carton.

THE END