TR-NPI-102

产品简介 General Information

- TR-NPI-102是一款通用型自由基光引发剂，常作为TR-BP的改进版使用。TR-NPI-102具有高引发效率、低气味的特性，广泛应用于食品包装油墨和光油。

- TR-NPI-102 is a general free radical photoinitiator, often used as an improved version of TR-BP. It’s high initiation efficiency and low odor. It’s widely used in food packaging ink and varnish.

产品信息 Product Information

- 化学名称 Chemical Name：3-甲基4-苯基二苯甲酮 3-Methyl-4-phenylbenzophenone

- 分子量 Molecular Weight：272.34

- CAS No：86428-83-3

紫外吸收光谱 UV Absorbance Spectrum

技术参数 Technical Parameters

- 外观 Appearance：类白色至白色粉末 Off-white to white powder

- 纯度 Purity (HPLC)：≥99.00%

- 熔程 Melting Range：81.0~84.0ºC

- 干燥失重 Loss on Drying：≤0.50%

产品优势 Benefits

- 高反应活性 High reactivity

- 低气味 Low odor

应用 Applications

- TR-NPI-102广泛应用在食品包装油墨和光油。建议添加量为3~5%。

- TR-NPI-102 is widely used in food packaging ink and varnish. The recommended dosage is 3~5%.

存储及包装 Storage & Packaging

- 保存在密闭容器中储存在阴凉、干燥、阴暗、通风的区域。自生产日期开始，1年内有效。包装：20kg/箱。

- Keep in a tightly closed container and store in a cool, dry, dark, ventilated area. Effective from the date of production, within 1 year. Packaging: 20kg/carton.

THE END