TR-369

产品简介 General Information

- TR-369是一款通用型自由基光引发剂，具备高引发活性和优秀的深层固化性能，常作为TR-907的替代品使用。TR-369可与其他光引发剂搭配使用，尤其是和硫杂蒽酮协同使用时，特别适用于有色体系的光固化。

- TR-369 is a free radical photoinitiator with high initiating activity and excellent deep curing performance, usually used as a substitute for TR-907. TR-369 can be used in combination with other photoinitiators, especially suitable for colored curing when used with thioxanthone.

产品信息 Product Information

- 化学名称 Chemical Name：2-苄基-2-(二甲基氨基)-1-（4-吗啉苯基）-1-丁酮 2-Benzyl-2-(dimethylamino)-1-[4-(4-morpholinyl)phenyl]-butanone

- 分子量 Molecular Weight：366.51

- CAS No：119313-12-1

紫外吸收光谱 UV Absorbance Spectrum

技术参数 Technical Parameters

- 外观 Appearance：淡黄色粉末 Light yellow powder

- 纯度 Purity (HPLC)：≥98.00%

- 熔程 Melting Range：110.0~123.0ºC

- 干燥失重 Loss on Drying：≤0.30%

产品优势 Benefits

- 高反应活性 High initiating activity

- 长吸收波长 Long absorption wavelength

- 优秀的深层固化性能 Excellent deep curing performance

应用 Applications

- TR-369可用于直接替代TR-907，建议添加量为3~5%。当和硫杂蒽酮协同使用时，例如TR-DETX，特别适用于有色体系的光固化。

- TR-369 can be used to directly replace TR-907; the recommended dosage is 3~5%. It’s especially suitable for colored curing when used with thioxanthone as TR-DETX.

存储及包装 Storage & Packaging

- 保存在密闭容器中储存在阴凉、干燥、阴暗、通风的区域。自生产日期开始，1年内有效。包装：20kg/箱。

- Keep in a tightly closed container and store in a cool, dry, dark, ventilated area. Effective from the date of production, within 1 year. Packaging: 20kg/carton.

THE END